SECTION 03450 - Architectural Precast Concrete

- GENERAL

  - DESCRIPTION

    - Section Includes :

      - Structural design and detailing of panels (products).

      - Plant fabrication of architectural precast concrete panels.

      - Transportation of precast panels to job site.

      - Installation of precast panels.

    - Related Documents : The requirements of the General Conditions, Supplementary General Conditions and applicable portions of Division 1 of these Specifications as they apply to this Section.

    - Related Sections :

      - Section 03200 - Concrete Reinforcement

      - Section 03415 - Precast Prestressed Concrete

      - Section 05500 - Metal Fabrications

      - Section 07920 - Sealants and Caulking

  - REFERENCES

    - California Building Code, 2019 Edition.

    - PCI MNL-120-17 : PCI Design Handbook, Precast and Prestressed Concrete, Eigth Edition

    - PCI MNL-117-13 : Manual for Quality Control for Plants and Production of Architectural Precast Concrete Products

    - PCI MNL-116-99 : Manual for Quality Control for Plants and Production of Structural Precast Concrete Products

    - AWS D1.1-98 : Structural Welding Code - Steel

    - AWS D1.4-92 : Structural Welding Code - Reinforcing Steel

    - ASTM A27 : Steel Castings, Carbon, for General Application

    - ASTM A36 : Structural Steel

    - ASTM A47 : Ferritic Malleable Iron Castings

    - ASTM A53 : Pipe, Steel, Black and Hot-Dipped, Zinc-Coated Welded and Seamless

    - ASTM A108 : Steel Bars, Carbon, Cold-Finished, Standard Quality

    - ASTM A123 : Zinc Coatings on Iron and Steel Products

    - ASTM A153 : Zinc Coating (Hot-Dip) on Iron and Steel Hardware

    - ASTM A184 : Fabricated Deformed Steel Bar Mats for Concrete Reinforcement

    - ASTM A185 : Steel Welded Wire Fabric, Plain, for Concrete Reinforcement

    - ASTM A307 : Carbon Steel Bolts and Studs, 60,000 Tensile Strength

    - ASTM A325 : Structural Bolts, Heat Treated, 120/105 ksi Minimum Tensile Strength

    - ASTM A416 : Steel Strand, Uncoated Seven-Wire for Prestressed Concrete

    - ASTM A449 : Quenched and Tempered Steel Bolts and Studs

    - ASTM A496 : Steel Wire, Deformed, for Concrete Reinforcement

    - ASTM A497 : Steel Welded Wire Fabric, Deformed, for Concrete Reinforcement

    - ASTM A500 : Cold-Formed Welded and Seamless Carbon Steel Structural Tubing in Rounds and Shapes

    - ASTM A563 : Carbon and Alloy Steel Nuts

    - ASTM A615 : Deformed and Plain Billet-Steel Bars for Concrete Reinforcement

    - ASTM A706 : Low-Alloy Steel Deformed Bars for Concrete Reinforcement

    - ASTM B633 : Electrodeposited Coatings of Zinc on Iron and Steel

    - ASTM B766 : Electrodeposited Coatings of Cadmium

    - ASTM C33 : Concrete Aggregate

    - ASTM C150 : Portland Cement

    - ASTM C260 : Air-Entraining Admixtures for Concrete

    - ASTM C979 : Pigments for Integrally Colored Concrete

    - DOD-P-21035

  - SYSTEM DESCRIPTION

    - Plant fabricated precast panels consisting of architectural concrete, steel reinforcement, steel connections for panel attachment to structure.  Panels are transported to the job site for installation.

    - Precast panel fabrication shall include all labor, materials, and equipment necessary to manufacture the panels as shown by the Contract Documents.

    - Precast panel installation shall include all labor, materials, and equipment necessary for the installation of the panels as shown by the Contract Documents.

    - The Precast Manufacturer shall design and furnish all precast connection hardware to be attached to or embedded in the panels; shall furnish all loose connection hardware, and shall furnish all connection hardware required to be embedded in the cast-in-place concrete for connection of the precast panels.  The placement of the hardware in the cast-in-place concrete will be the responsibility of the General Contractor.

    - Embeds and hardware which are to be cast into the precast panels for other trades shall be provided to the Precast Manufacturer, with instructions, in a timely manner in order not to disrupt or delay production.  All such embeds and hardware shall be fully defined in contract drawings.

    - When required by the Contract Documents, the Precast Manufacturer shall design, furnish, and install steel pre-weld required (such as clip angles and drop tubes) to carry the loads from the precast panels to the structure.  Any bracing or stiffening of the structure required to support the loads from the precast panels shall be by others.

  - QUALIFICATIONS

    - Design : Precast panels shall be designed under the supervision of a civil engineer registered in the State of California employed or retained by the Precast Manufacturer, using the accepted principles of design as stipulated in the PCI Design Handbook, Precast and Prestressed Concrete MNL-120.  All design loads shall meet the requirements of the California Building Code, 2019 edition.

    - Manufacturing : The precast manufacturing plant shall be certified at the time of bid by the Precast/Prestressed Concrete Institute Plant Certification Program for Group AA.

Acceptable Manufacturers :

- Willis Construction Co., Inc.

    - Erector : Regularly engaged for at least 5 years in erection of architectural precast panels similar to those required on this project.  The present erection management team shall be capable of installing the required panels without causing delay of project schedules.

    - Welders (Shop, Plant and Field) : Welders performing work under this specification shall be qualified in accordance with AWS D1.1, and AWS D1.4 as required to perform work at all stages of production and erection.

    - Testing : Precast Manufacturer shall comply with the testing provisions in MNL-117, Manual for Quality Control for Plants and Production of Architectural Precast Concrete Products.

  - SUBMITTALS

    - Samples :

      - Submit preliminary samples, approximately 12" by 12", representative of finished exposed face.

      - Prior to commencement of manufacture, submit production samples, approximately 4' x 4', for final approval of colors and textures.

    - Shape and Erection Drawings : Submit one (1) electronic file of set showing;

      - Material specifications,

      - Floor plans identifying location of panels,

      - Floor plans and/or elevations identifying location of pre-erection attachments (i.e. cast-in-place embeds and prewelds) to support structure,

      - Elevations identifying location of panels and their connections,

      - Details as necessary to describe relationship of panels to adjacent material,

      - Details of panel connections,

      - Description of all panel connection hardware.

      - Elevations and sections of typical panels showing;

        - geometry and finish,

        - thickness of face and back-up mixes (if applicable),

        - reinforcement layout,

        - stripping, lifting, and erection insert sizes and locations,

        - embeds with piece marks and their locations.

    - Mix Designs : Submit all precast mix designs for approval.  Mix designs shall be prepared by an independent testing facility or qualified employee of the Precast Manufacturer.

    - Weld Procedure Specifications : Submit Welding Procedure Specifications in accordance with AWS D1.1 and D1.4 requirements for all welding which will be performed under this Section.

    - Design Calculations : Submit complete design calculations for governing panel types and connections, including loads used in design.

    - Design Modifications :

      - Submit design modifications necessary to meet performance requirements and field conditions.

      - Variations in details or materials shall not adversely affect the appearance, durability or strength of panels.

      - Maintain general design concept without altering size of members, profiles and alignment unless otherwise approved by the Architect/Engineer.

  - QUALITY ASSURANCE

    - Full-Scale Panel :

      - After standard samples are accepted for color and texture, produce full-scale panel meeting design requirements.  This panel shall be viewed and approved by the Architect at the precast plant.

      - The full-scale panel shall be representative of standard quality for precast panel work, when accepted by Architect.

      - Incorporate full-scale panel into work after keeping panel in plant for checking purposes.

    - In-Plant Quality Control

      - The Precast Manufacturer shall have an established PCI quality control program in effect prior to bidding.  If requested, a copy of this program shall be submitted to the Architect.

      - Testing of materials and inspection of production methods shall be the responsibility of the Precast Manufacturer’s Quality Control Department and performed in accordance with PCI MNL 117.

      - Keep quality control records available for two years after final acceptance.

      - Keep certificates of compliance available for five (5) years after final acceptance.

    - All other testing and inspection, including 3rd Party, to be provided by Owner.

- PRODUCTS

  - PRECAST CONCRETE MATERIALS

    - Portland Cement

      - Architectural Mixes : ASTM C150 Type I, II or III cement.  For surfaces exposed to view when the building is complete use same brand, type and source of supply throughout the precast production.

      - Back-up Mixes : When used, the back-up mix shall be compatible with the  architectural mix to which it is combined.

    - Aggregates : Fine and coarse aggregate for mix shall conform to ASTM C33 except for gradation.  Aggregates shall be clean, hard, strong, durable, inert, and free of staining and deleterious materials.

    - Water : Free from deleterious matter that may interfere with the color, setting, or strength of the concrete.

    - Admixtures : Conforming to ASTM C260 and/or ASTM C494.

    - Coloring Agent: Conforming to ASTM C979.

      - Shall be harmless to precast concrete set and strength,

      - Shall be stable at high temperatures,

      - Shall be alkali-resistant.

    - Concrete Strength : Concrete strength shall be determined by design with a minimum 28 day design strength of 5,000 psi.

  - STEEL PRODUCTS

    - Structural Shapes, Bars & Plates (1/8" and thicker)	ASTM A36

    - Pipe	ASTM A53 Grades A or B

    - Tube Steel	ASTM A500 Grades A or B

    - Reinforcing Steel	ASTM A615 Grades 40 & 60 or ASTM A706

    - Prestressing Strand	ASTM A416 Grade 270

    - Deformed Steel Bar Mats	ASTM A184

    - Deformed Bar Anchors	ASTM A496

    - Deformed Welded Wire Fabric	ASTM A497

    - Plain Welded Wire Fabric	ASTM A185

    - Welded Headed Studs	AWS D1.1 Type B

    - Standard Machine Bolts	ASTM A307 Grade A

    - Standard Studs/Threaded Round Stock (UNC) … ASTM A307 Grade C

    - Nuts for Standard Machine Bolts and Threaded Studs … ASTM A563 Grade A Hex Nuts

    - High Strength Machine Bolts … ASTM A325 Type 1, ASTM A449 Type 1

    - Nuts for High-Strength Machine Bolts and Threaded Studs … ASTM A563 Grade A Heavy Hex Nuts

    - Coil Rods and Bolts	ASTM A108 - SAE 1016 to 1026, Fu/Fy = 70/55 ksi minimum

    - Coil Nuts for Coil Rods and Bolts … Nuts passing a proof load stress of 80 ksi, based on the tensile stress area of the matching coil rods and bolts.

    - Malleable Iron Castings	ASTM A47 Grade 32510

    - Carbon Steel Castings	ASTM A27 Grade 60-30

  - STEEL PROTECTIVE COATINGS : All connection hardware exposed to weather after completion of building shall be hot-dip galvanized.  All connection hardware not exposed to weather after completion of building may be uncoated, except as otherwise explicitly required by the contract drawings.  Fasteners can have either an electroplated zinc or cadmium coating.

    - Alkyd Rust Inhibitive Primers (shop primers such as red iron oxide) :

      - Tnemec Series FD88 Azeron Primer

      - Ameron 5105

      - 5275 DTM Low Sheen Primer/Finish

      - 1760 Alkyd Steel Primer

    - Zinc Coatings :

      - Hot-Dip Galvanizing	ASTM A123, or ASTM A153

      - Electroplated Zinc for Steel Products and Steel Hardware	ASTM B633

      - Zinc Rich Paints	DOD-P-21035

    - Cadmium Coatings :

      - Electrodeposited Coatings of Cadmium	ASTM B766

  - FABRICATION

    - Precast Manufacturer shall not proceed with fabrication of panels prior to receiving the approved set of Shop Drawings and the Architect’s acceptance of submitted Samples.

    - Manufacturing procedures shall be in general compliance with PCI MNL-117.

    - Batching of Concrete shall be in accordance with approved Mix Design(s).

    - Forms :

      - Forms for precast panels shall be rigid and constructed of materials that will result in finished products conforming to the profiles, dimensions and tolerances indicated by this Section, the Contract Documents and the approved Shop Drawings.

      - Construct forms to withstand vibration method selected.

      - Release agents shall be applied and used according to manufacturer's instructions.

    - Cover : Minimum concrete cover for rebar, inserts and embeds shall be 3/4", where applicable.

    - Concreting :

      - Convey concrete from the mixer to place of final deposit by methods which will prevent separation, segregation or loss of material.

      - Consolidate all concrete in the form to minimize unintentional pour lines, honeycombing or entrapped air on vertical surfaces.

    - Curing : Procedures sufficient to insure specified concrete strength of all precast panels must be employed.  Stripping of a panel shall not occur until concrete strength is sufficient to prevent cracking or breaking of the panel.

    - Manufacturing Tolerances :

      - Overall height and width of panels measured at the face exposed to view:

        - 10' or less	+/-1/8"

        - 10' to 20'	+1/8", -3/16"

        - 20' to 40'	+/-1/4"

        - Each additional 10'	+/-1/16"

      - Overall height and width of panels measured at the face not exposed to view:

        - 10' or less	+/-1/4"

        - 10' to 20'	+1/4",-3/8"

        - 20' to 40'	+/-3/8"

        - Each additional 10'	+/-1/8"

      - Variation from square or designed skew (difference in length of two diagonal measurements)	1/8" per 6' or 1/2" total, whichever is greater

      - Bowing: Bowing shall not exceed L/360 unless it can be shown that the member can meet erection tolerances using connection adjustments.

      - Length and width of blockouts and openings within one panel	+/-1/4"

      - Location of window opening within panel	+/-1/4"

      - Location of blockouts other than window openings	+/-3/8"

      - Warpage : Maximum permissible warpage of one corner out of the plane of the other three shall be 1/16" per foot distance from the nearest adjacent corner.

      - Location of bearing connections	+/-1/4"

      - Location of embeds and Inserts other than bearing connections	+/-1/2"

    - Panel Identification :

      - Mark each precast panel with corresponding to identification mark on Shop Drawings.

      - Mark each precast panel with casting date.

    - Panel Finish and Approval : Precast panels and approved Samples shall be viewed side by side from a distance of 20' when comparing texture and color.  Precast panels which do not reasonably match the color and texture of the approved sample(s), the dimensional tolerances, or industry standards may be rejected at the option of the Architect if they cannot be satisfactorily corrected.

- EXECUTION

  - PRODUCT TRANSPORTATION AND HANDLING

    - Handle and transport panels in a position consistent with their shape and design in order to avoid excessive stresses or damage.

    - Lift or support panels only at the points shown on the Shop Drawings.

    - Support panels during shipment on non-staining shock-absorbing material as needed to prevent damage.

  - PRE-INSTALLATION RESPONSIBILITY

    - General Contractor's Responsibility :

      - The General Contractor shall provide the control layout grid lines, and elevation benchmarks, at each building elevation on each floor receiving precast panels.

      - The General Contractor shall provide true, level, and clean support and attachment surfaces.

      - The General Contractor shall provide for the accurate (1/2" in all directions) placement and alignment of connection hardware on the structure.

      - The General Contractor shall be responsible for patching fireproofing after precast panel installation.

      - The General Contractor shall confirm that the dimensions and tolerances of the structure allows for proper installation of the precast panels.

    - Erector's Responsibility : Prior to installation of the precast panels, notify the General Contractor of any discrepancies discovered which affect the work under this contract.  Commencement of installation does not constitute acceptance of the structure.

  - ERECTION

    - Unloading Areas and Access : Clear all-weather unloading areas and access roadways around the building and in the building (where appropriate) shall be provided and maintained by the General Contractor so that the hauling and erection equipment for the precast panels may operate under their own power.

    - Safety Aspects : The General Contractor shall provide all required traffic controls, barricades, warning lights and/or signs to insure a safe installation.

    - Setting : Precast panels shall be lifted with suitable lifting devices at points provided by the Precast Manufacturer to prevent excessive stresses or damage to the panels.

    - Temporary Supports and Bracing : The erector shall provide temporary supports and bracing as required to maintain position, stability and alignment until panels are permanently connected.

    - Tolerances of Erected Panels : Tolerances for location of precast panels shall be as listed below;

      - Plan location from building grid datum	+/-1/2"

      - Top elevation from nominal top elevation :

        - Exposed individual panel	+/-1/4"

        - Nonexposed individual panel	+/-1/2"

        - Exposed relative to adjacent panel	1/4"

        - Nonexposed relative to adjacent panel	1/2"

      - Maximum plumb variation over height of structure or

100 ft. whichever is less	1"

      - Plumb in any 10 ft. of element height	1/4"

      - Maximum jog in alignment of matching edges	1/4"

      - Joint width (governs over joint taper)

        - Panel dimension less than 20'	+/-1/4"

        - Panel dimension over 20'	+/-3/8"

      - Joint taper maximum	3/8"

      - Joint taper in 10 ft.	1/4"

      - Maximum jog in alignment of matching faces	1/4"

      - Differential bowing as erected between

adjacent member of the same design	1/4"

    - Final Connection of Panels to Structure :

      - Precast panels shall be attached to the structure as shown on the approved Shop Drawings.

      - All modifications made to details shown on Shop Drawings shall be submitted for approved.

      - Welding shall not be performed prior to receipt of the approved submitted Weld Procedure Specifications.

    - Connection Verification : The Erector shall verify that all connections are executed per the approved Shop Drawings.

  - JOB SITE STORAGE, HANDLING, AND PROTECTION :

    - Erector shall be responsible for the repair of damage to precast panels that is caused by its own crew.

    - After precast panels are installed in their final positions, the General Contractor shall be responsible for their protection.

    - The General Contractor shall be responsible for the repair of any damage to the precast panels caused by someone other than the Precast Manufacturer.

  - PATCHES AND REPAIRS :

    - Patching of panels, when required, shall be performed to the Architect's satisfaction and consistent with industry standards.

    - Repairs shall be sound, permanent and flush with adjacent surface.

    - From a distance of 20' all repairs must be of color and texture matching adjoining surfaces and showing no apparent line of demarcation between original and repaired work.

  - CLEANING :

    - Cleaning methods shall be approved by Precast Manufacturer.

    - Erector shall clean erection marks from precast panels, when exposed to view, when the building is complete.

    - Precast Manufacturer is responsible for providing a clean panel to Erector.

    - Use care to prevent damage to precast surfaces and to adjacent materials.

    - Surface must be thoroughly rinsed with clean water immediately after using cleaner.

    - At completion of the project, General Contractor shall be responsible for final cleaning and wash down of building.

  - SEALER AND/OR ANTI-GRAFFITI (where used) :

    - Seal exposed precast surfaces, where indicated on contract drawings, with one coat of water repellant coating in accordance with product manufacturer’s recommendations  and Section 07920 - Sealants and Caulking.

    - Surfaces to be free of dirt, dust, and other foreign material immediately prior to sealer application.  Precast Manufacturer, at his option, may factory apply sealer.

    - Patches or other work on panel surfaces which have removed sealer shall be resealed by the responsible party.

  - INSPECTION AND ACCEPTANCE : Immediately after installation is completed, final inspection and acceptance of the installed precast panels shall be made by the Architect and General Contractor to verify conformance with plans and specifications.  In cases where precast panel installation is phased, panels shall be inspected and approved in phases.

  - WARRANTY : All labor and materials under the Precast Manufacturer’s contract shall be warranted by the Precast Manufacturer for a period of one (1) year following final approval of the precast panel by the Architect.  Any additional labor or material warranties, i.e. caulking, shall be passed through to the General Contractor with no responsibility by the Precast Manufacturer.

END OF SECTION